	[bookmark: _GoBack]Scream4_M_01_black
	
	Prussian blue, carbonyl at 1740 cm-1, strong signals of the paper support that are modify in the 1200-1000 cm-1 by the unassigned contribution

	Scream4_M_02_paper
	
	signals of the paper support

	Scream4_M_03_green
	
	Prussian blue, lead chromate-sulphate, the signals of the paper are evident except in the range 1200-1000 cm-1 where also gum may contribute

	Scream4_M_04_black
	see the image corresponding to the area, no evident blue area but mainly black, although this the signal of Prussian blue are evident
	Prussian blue, carbonyl at 1740 cm-1, strong signals of the paper support that are modify in the 1200-1000 cm-1 by the unassigned contribution

	Scream4_M_05_nero
	area with blue spots (see corresponding ALPHA camera image)
	Prussian blue, carbonyl at 1740 cm-1, strong signals of the paper support that are modify in the 1200-1000 cm-1 by the unassigned contribution

	Scream4_M_06_yellow
	Yellow area on black ground check by XRF
	Prussian blue, no carbonyl at 1740 cm-1, the signals of the paper are evident except in the range 1200-1000 cm-1 where also gum may contribute

	Scream4_M_07_nero
	black with blue spots, 
	Prussian blue, carbonyl at 1740 cm-1, strong signals of the paper support that are modify in the 1200-1000 cm-1 by the unassigned contribution

	Scream4_M_08_paper
	
	signals of the paper support

	Scream4_M_09_red
	check by XRF low spatial resolution also the black areas may contribute
	Prussian blue (very weak),weak carbonyl at 1740 cm-1(as a shoulder), the signals of the paper are evident except in the range 1200-1000 cm-1 where also gum may contribute, inverted band at 340 cm-1

	Scream4_M_10_red
	
	Prussian blue (very weak), no carbonyl at 1740 cm-1, the signals of the paper are evident except in the range 1200-1000 cm-1 where also gum may contribute, inverted band at 340 cm-1

	Scream4_M_11_blue
	blue on the white support but close to black line
	Prussian blue, no carbonyl at 1740 cm-1, the signal of the paper 

	Scream4_M_12_black
	black are with no evidence of the blue spot
	Prussian blue, carbonyl at 1740 cm-1, strong signals of the paper support that are modify in the 1200-1000 cm-1 by the unassigned contribution

	Scream4_M_13_black
	clearly absent any traces of blue
	Prussian blue, carbonyl at 1740 cm-1, strong signals of the paper support that are modify in the 1200-1000 cm-1 by the unassigned contribution

	Scream4_M_14_yellow
	pale yellow
	carbonyl band at 1740-36cm-1, signal of the paper modified by unassigned features in the 1200-1000 cm-1

	Scream4_M_15_yellow
	transparent yellow
	carbonyl band at 1740-36cm-1, signal of the paper modified by unassigned features in the 1200-1000 cm-1

	Scream4_M_16_brown
	low spatial resolution probably also black sourronding areas may contribute
	no carbonyl, only the signal of the paper

	Scream4_M_17_yellow
	transparent yellow
	carbonyl band at 1740-36cm-1, signal of the paper modified by unassigned features in the 1200-1000 cm-1



