UV-Vis reflectance

| G0193-03_R_01_red |  | sigmoidal shape with an inflection point at about 595 nm,consistent with mercury sulfide (to be confirmed with XRF) |
| --- | --- | --- |
| G0193-03_R_02_light red | possible light HgS check XRF | weak sigmoidal shape with an inflection point at about 585 nm, possibly related to diluted mercury sulfide (to be confirmed with XRF) |
| G0193-03_R_03_red |  | sigmoidal shape with an inflection point at about 595 nm, consistent with mercury sulfide (to be confirmed with XRF) |
| G0193-03_R_04_yellow | spot with more dense color but very small | broad sigmoid with and inflection at about 470 nm |
| G0193-03_R_05_paper |  |  |
| G0193-03_R_06_yellow |  | broad sigmoid with and inflection at about 470 nm |
| G0193-03_R_07_yellow | spot with more dense color but very small | broad sigmoid with and inflection at about 415 nm - light yellow |
| G0193-03_R_08_green |  | Possible prussian blue mixed with yellow pigment otherwise green copper-based pigment |
| G0193-03_R_09_blue |  | Prussian blue |
| G0193-03_R_10_blue | check with mid-FT-IR the spot is small so the measure is difficult | Prussian blue |
| G0193-03_R_11_brown | check XRF and Mid FT-IR | inflection at 580 nm and a large and weak absorption band centered at 700 nm; could be prussian blue + HgS |
| G0193-03_R_12_brown | check XRF and mid FT-IR | inflection at 580 nm and a large and weak absorption band centered at 700 nm; could be prussian blue + HgS |
| G0193-03_R_13_orange |  | sigmoidal shape with an inflection poiny at 583 nm, quite close to the red paint in Scream 5 (minium); XRF could provide the identification; possible Prussian blue |
| G0193-03_R_14_yellow | thick yellow pigment over black | sigmoidal shape with two inflection points at 524 and 578 nm yellow component: cadmium based pigment (NIR fluorescence) red component: possibly the same present in the orange area (check XRF for Hg or Pb) |
| G0193-03_R_15_yellow | thicker paint over black line | very small area sigmoidal shape with two inflection points at 502 and 585 nm yellow component: no clear evidence of NIR fluorescence red component: possibly the same present in the orange area (check XRF for Hg or Pb) Possible Prussian blue |
| G0193-03_R_16_green |  | viridian |
| G0193-03_R_17_green |  | Possible prussian blue mixed with yellow pigment otherwise green copper-based pigment |

UV-vis fluorescence

| g0193-03_F_01_red |  | no emission |
| --- | --- | --- |
| g0193-03_F_02_light red | contribution from paper | no emission |
| g0193-03_F_03_red |  | no emission |
| g0193-03_F_04_yellow |  | no emission |
| g0193-03_F_05_paper | signal from paper to be compared with the other areas |  |
| g0193-03_F_06_yellow |  | no emission |
| g0193-03_F_07_yellow |  | no emission |
| g0193-03_F_08_green | check for cadmium | very low near infrared emission - possible presence of a cadmium-based pigment |
| g0193-03_F_09_blue | to compare with f_08_green | no emission |
| g0193-03_F_11_brown |  | no emission |
| g0193-03_F_13_orange |  | weak signal in the NIR |
| g0193-03_F_14_yellow |  | cadmium based pigment; emission at 770 nm - CdS |
| g0193-03_F_15_yellow |  | very low near infrared emission - possible presence of a cadmium-based pigment |