| Scream1_M_01_white | faded area | kaolin, carbonyl at 1740 cm-1, signals of cardboard |
| --- | --- | --- |
| Scream1_M_02_cardboard | colored paint might be also present. | Kaolin (less evident with respect to M01), no presence of carbonyl band at 1740 cm-1, signals of cardboard |
| Scream1_M_11_yellow | Intact yellow area. Less thick brushstrock | cadmium carbonate, Cd(OH)Cl (very weak),carbonyl at 1740 cm-1,possible oxalates |
| Scream1_M_12_yellow |  | cadmium carbonate, Cd(OH)Cl,carbonyl at 1740 cm-1, possible oxalates |
| Scream1_M_13_orange |  | zinc oxalates, Cd(OH)Cl not evident, Sulfates?, carbonyl band at 1740 cm-1, band at 2470 cm-1 |
| Scream1_M_14_orange |  | zinc oxalates, Cd(OH)Cl not evident, Sulfates?, carbonyl band at 1740 cm-1 (CH lipidic), Prussian blue |
| Scream1_M_15_orange | no Cd from XRF mapping | no oxalates, CaCO3, weak kaolin, carbonyl band at 1740 cm-1, sulphates (lead) |
| Scream1_M_16_yellow | Pb, Cr from XRF mapping | mainly kaolin, carbonyl, |
| Scream1_M_17_red | Hg by XRF mapping | kaolin, carbonyl band at 1740 cm-1 and sharp CH strecthing (lipidic component) |
| Scream1_M_18_blue | area that is dark in the reflectography at 850 nm by INO | ultramarine blue, oxalates (Zn), weak kaolin, carbonyl band at 1740 cm-1 |
| Scream1_M_19_blue | area that is transparent in the reflectography at 850 nm by INO | ultramarine blue, oxalates (Zn), weak kaolin, carbonyl band at 1740 cm-1 |
| Scream1_M_20_black |  |  |
| Scream1_M_03_cardboard | cardboard close to the white point M01 defined faded by conservators. | Kaolin (less evident with respect to M01), no presence of carbonyl band at 1740 cm-1, signals of cardboard. Kaolin intensity similar to M02 |
| Scream1_M_21_white | white line considered by conservators as faded yellow | cadmium carbonate, kaolin, carbonyl at 1740 cm-1. |
| Scream1_M_22_white | white line considered by conservators as faded yellow | cadmium carbonate, kaolin, carbonyl at 1740 cm-1. |
| Scream1_M_23_yellow | continuation of the white faded line the same yellow also investigated by fluorescence spectroscopy poin F01 | cadmium carbonate, kaolin, carbonyl at 1740 cm-1. |
| Scream1_M_24_yellow | yellow close to point F09 | Cd(OH)Cl, Cd carbonate,carbonyl at 1740 cm-1 |
| Scream1_M_25_blue |  | carbonyl at 1740 cm-1, oxalate (likely Zn), Zn oxide, carbonates (cadmium) |
| Scream1_M_26_black |  | ultramarine, carbonyl at 1740 cm-1 |
| Scream1_M_27_red | measurement close to F17 | carbonyl at 1740 cm-1, band at 1470 cm-1 |
| Scream1_M_28_cardboard | stain | sulphates |
| Scream1_M_29_cardboard | likely original colour | signals of cardboard |
| Scream1_M_30_cardboard | whitened cardboard due to water | signals of cardboard |
| Scream1_M_04_white | white exudate over cardoboard | Kaolin (signals more intense than M01), signals of cardboard |
| Scream1_M_31_cardboard | stain | sulphates |
| Scream1_M_32_blue | XRF: blue paint with zinc | ultramarine, zinc oxalates, possibly Co-based blue, carbonyl 1740 cm-1, CH combination bands of lipid |
| Scream1_M_33_blue | XRF: blue paint with no zinc | ultramarine, carbonyl 1740 cm-1, CH combination bands of lipid, calcium carbonate, weak kaolin |
| Scream1_M_34_green |  | zinc oxide, cadmium carbonate, Cd(OH)Cl, zinc oxalates, kaolin, carbonyl 1740 cm-1 |
| Scream1_M_35_white | possibly faded yellow paint | cadmium carbonate, kaolin |
| Scream1_M_36_yellow | yellow paint continuation of the white faded brush | cadmium carbonate |
| Scream1_M_37_orange | closer to M_15 but no clear evidence of lead sulfate | weak oxalates, carbonyl 1740 cm-1, CH combination bands lipide-like, inverted bands at 1030 and 593 cm-1 |
| Scream1_M_05_blue | white exudate over blue paint | kaolin, carbonyl at 1740 cm-1, signals of cardboard |
| Scream1_M_06_blue | area close to M05 but without presence of exudate | ultramarine, kaolin (very weak signals), possible oxalates |
| Scream1_M_07_purple | no elemental keys by XRF, check by NIR | kaolin (weak), carbonyl at 1740 cm-1, ultramarine, sharp CH bending (paraffin?) |
| Scream1_M_08_green | check presence of viridian by reflectance UV-Vis. | carbonyl at 1740 cm-1, signals of cardboard, kaolin (very weak), possible viridian |
| Scream1_M_09_yellow | Region with loss of paint. The region of interest is smaller than the spot size of the source. | kaolin, signals of cardboard |
| Scream1_M_10_yellow | Intact yellow area. The region of interest is smaller than the spot size of the source. | carbonyl at 1740 cm-1, cadmium carbonate, possible oxalates, Cd(OH)Cl,possible oxalates |